construction - deck - # 1

fashion according to the offset table & deck drawing

the deck out of 20mm / 3/4" polydur / dow 4% densisty foam ....

making a structural clue joint on every  line  shown

to transmit the stress from one side of the foam to the other ....

building it on a flat surface possibly in 2 half sections

as shown on the deck drawing

with a plastic foil under so it will not stick onto ...

note that under each future frame

should be a 20mm / 3/4" square stick of foam

clued on with a thick structural mixture of glass fibers

so that the frame loads are carried to the deck  later on

and beyond to the bridge deck top extension stations  #C - Ca - 0 - 0a - 1 - 1a - 2 - 2a - 3 - 3a ....

except under the mast step being 18" from the center of the hull

a square 20mm / 3/4" piece of douglas fir grain high up ...

then you put on as well strips on the borders of the decks all  yellow area

to cover the  deck area beyond the frames

from the 20mm / 3/4"  planking of the hull later on as well ...

after drawing on the  # of each frame to be put on later with a felt pen

brush on a mirco balloon epoxy mixture to the entire deck

and then lay down the prefashioned  6oz glass

to soack up the epoxy ....

try out this procedure so you will have just enough mixture

to have the cloth wetted wholely

but not any more then neccessary to save on weight ...

fritz.roth@proadesign.com