# 2 construction frames and planking

fashion out of 20mm styrodur  / 3/4" dow 4% densisty foam

the frames # C - # 0 - # 1 - # 6 - # 7 - # 8

according to the frames drawing & offset table

up to the main deck level

& over to the lite blue bridge deck area

# C - # 0 - # 1 ...

joining the two as in the deck construction

with structural mixture

having a 20mm styrodur  / 3/4" dow 4% densisty foam insert between

as well as a triangular piece below them ....

and marking on the main cut outs on the  # C - #0 & #1 frames

but leave the parts on untill planking has been completed  ...

except the center only cut outs on #0

and # 6 if you desire one

for ventilation via the forward hatch ...

then brush on a micro baloon mixture

onto the inboard side

of # C - # 0 - # 1 - # 6 - # 7 - # 8

and put on the precut glass

put on another layer onto this

roll over with a roller

to have the epoxy soak into the cloth all the way ...

except where you have a cut outs !

after hardening do the bow side

but only on # C - # 0 - # 1

remove the excess cloth later on

with a disk sander up to your felt pen line ...

then put them up square on the deck

with a bead of structural mixture on both sides

to mate the joints there .....

if you build the hull in 2 halfs be especially carefull in aligning the # C

since it will on mating with the other halfs # C

determain the shear of the finished boat !

shape the out ward frames after hardening

on the bow side to fit the hull shape ...

the building frames # 2 to 5 of the main hull

you can build out of foam too ...

even only half frames and only one of them

if you change them where you are just then planking on ....

fill in the spaces between the #C #0 #1 & #1a stations

with 20mm styrodur  / 3/4" dow 4% densisty foam

as shown in the seat drawing out towards the later long wing profile

and glass as usual the now top side inside the main hull

and out to the bridge deck

as well as up on the main hull frames what will be there

when you cut the cloth to fit ...

put 2x strips of glass tape on the perimeter of the frames #C #0 & #1

according to the strips drawing just tacking them onto as shown ....

put on the 3/4" wide keel up to the stem fashined according to the offset table

then put on the planking of 20mm foam / 3/4" dow 4% densisty foam

starting from the #1a towards with 6" wide from the deck upwards  ....

except between the #C & #0 # 1 & #1a for 6" on up from the deck

then use 2x 4" wide all the lenght of the hull

then 2x 2" wide strips of planking

then down to a 1" size to have a round hull on to the keel ....

see the strips drawing for details .....

shape each strip to fit onto the previous

by cutting it at a bevel and sanding it later !

then clue them together up to the whole lenght

before putting them on to the frames

bevel the stem ends too first ...

be shure to get no epoxy onto the hull out side

or even close to

since it will make it impossible to sand off an even surface

but a clue bead should join to each structural glas side on the frames .....

if you have build the hull in 2 halfs

join the hull halfs together according to the strips drawing

leaving the last foot before the end with out any structural mixture

since a perpared fiber glass tape will have to be inserted later there

for joining to the fin ......

prepare the the deck by using a open blade hack saw as shown

fill every thing with structural mixture and clamp together

now you can glass the hull on one side

+ a layer on the other side

overlaping each a couple of inches

then again

then two more on from the wl all over

+ covering the stem about 4" each side

and the last one a little smaler ...

all by laying as usual the precut glas onto your coated hull

and letting it soak up all while wet ....

now fashion out of 20mm styrodur  / 3/4" dow 4% densisty foam

the bridge deck frames

# 0a - # 1a - # 2 - # 2a - #3 - # 3a

according to the frames drawing

up to the main deck level  & only over  the lite blue bridge deck area ...

then cut out a 1x2" slot on the # 3 bridge deck frame

and replace with 20mm / 3/4" high up grain douglas fir

for the mast step to mate onto ....

now glue them onto the bridge deck part as shown in the deck drawing

and tape to the main hull glass planking

already there !

and cover the rest of the bridge deck under cover

almost out to the long wing profile

with 20mm styrodur  / 3/4" dow 4% densisty foam

then glass out from the main hull to about 6" before the end of the panels

since these panels are partly curved

use the methode shown in the bending drawing for the proper fit !

then put on the bevel part planking as shown in the triangular area

at the joining of hull and bridge deck ...

fritz.roth@proadesign.com