# 3 construction fin frames

fashion out of 20mm styrodur foam

/ 3/4" dow 4% densisty foam

the # C fin frames according to the fin frames drawing

up to white part

this being the lee side of long wing profile ...

insert the usual 20mm / 3/4" pieces with structural mixture

for later supporting the fin deck

fin profiles and wing profiles ...

brush on a mircro ballon mixture on one side

and lay down a prefashioned cloth

lay down another one up to half way up to arm

then do the other side later ....

if you have been building inside a garage

you may as well want to build the whole fin part there

for this you lay down the #C frame onto your perfectly level platform

and assemble the profiles and the next frames

onto there all upwards perfectly square !

each half as the mirror of the other as described in the text below ......

then put them together with structural mixture except for the last foot

before the long profile !

since we need to insert a thin piece of previously cured fiberglass

on assembly with the hull section .....

now turn over the main hull and raise up 18" from the ground

supporting it so it is level on both axis ....

clue onto the # C frames

the deck profile being 6" below the lower hull deck level

as shown on the fin frames gif

by adjusting the bottom of the fin more or less above the ground ...

by preparing the ends of the frames as shown in the junction drawing

with the foam removed with an open end hack saw

and having cured 4" long piece of double 1"1/2 fiber glass tapes

inserted between at the main hull #C frames where shown on > junction <

and pushed with a 3" putty blade

a doubled up 4" long 1"1/2 fiber glass tape into the foam slots where shown !

all with structural mixture wetted down .......

so the #C will be vertical and at right angle

by measuring from the main bows to the frame top

and the fin bottom the same lenght each ...

lay down a board at the inside of the fin bottom

and align exactly with the keel line of the main hull ....

make and install the deck & bottom profile section

between # C & # 0 ....

then make 2 x more fin frames as # 0

shown in the fin profile drawing ....

install the two frames according to the above

with glassed profile sections of 7"1/4 long

at each of the 20mm / 3/4" inserts

the other dimension being the same as on the frames ....

the glass being left off

on the bottom of the bottom profile at this time ....

make and install the deck & bottom profiles

between # 0 & # 0a ....

then make 2 x more fin frames as # 0a

shown in the fin profile drawing ...

then install the two frames according to it

with glassed profile sections of 7"1/4 long

at each of the 20mm / 3/4" inserts

the other dimension being the same as on the frames ....

fritz.roth@proadesign.com