# 4 construction fin & wing profiles

fashion out of 20mm / 3/4" dow 4% densisty foam

the remaining fin profile parts

shown in the > profile drawing

glass on the top & bottom

but make the lower part shorter for c & d

as shown in the > fin side drawing before or after glassing ...

then install on the frames ....

then make the wing profile parts to go between the frames

and glass on both sides

but make the lenght of the sides unequal as shown ...

install the shorter one

and put the longer one aside for now

till the #C -  # 0 & #0a  frames have been glassed over

as soon as the bridge deck top frames have been installed ...

shape the previously installed deck profile between # C - #0 & #0a

on the wing side according to the profile drawing now

then fill in all surfaces with 20mm  / 3/4" dow 4% densisty foam

up to the short wing profile ...

let the bottom wing planking

go all the way into between the # C - # 0 & # 0a frames too

leaving the fin planking between the c profile

as well as the 45° wing root off ..

these will be installed after the wing planking

has been glased on the bottom

as well as to the frames later

when upside down .....

it is best to clue on the wing foam planking an the # 0 first

then bend down and shape the mating surfaces to the bottom twin ....

since this should be bend to form a foil

glue the panel onto the last frame first > #0

then after hardening bend it on down

shaping the mating surface to the other

being top and bottom panels

apply glue and hold both together

till the new mixture hardens ....

what you can not bend

shape afterward ....

see also the bending sketch

for a way to permanetly bend the foam

so you will have the shape done before installing !

take a 3/4" radius off the deck and 3/8" on wing now

then glass 3x the outside of the fin down to the d profile

wrapping around the corners .....

fritz.roth@proadesign.com