vfp 25 mc                                                  fritz.roth@proadesign.com

general construction notes

>>> first check out your 2x4' - 60x125cms foam panels weight

with a kitchen scale

it should be around 1# 5oz - 600grs

if it has over 1#7oz - 650grs or under 1# 3oz - 550grs

you bought the wrong foam !

>>> when planking the wing it will be better if you pre bend the panels involved

so see bending.gif

putting down on the concrete floor the 1x4" - 20x100mms lumber as shown

then lay your 8" wide foam panel over it and put your knie on it to preload

then punch it at 2" intervals with a short bromhandle or similar

in about 3 rows with you hammer to keep the bend for good !

check if it suites your application and increase the curve if needed .....

>>> I recommend using an ultra violet resistant epoxy systems

for a final coat !

and titanium dioxide power mixed into the resin first

from the arts supply !

for any pale tint you can add a little of a paste for epoxy systems

but it should not be too much

since it may degrade its strenght .....

but if you want to have paint

then only real 2 component epoxy should be used

and as well only lite colors

since a dark surface will heat up the structure

in sun light

and may damage the epoxy under .....

>>> some foam supplies are very rough at the finish

so sanding is required or you will be using too much epoxy in the voids

some others are too shiny and nothing will hold to them

but be careful and use a hard sanding block like a piece of  foam

so you will not take off more at the foam then the joints

>>> on curvature like the frames or the wing

you need to mark down the reference points first

then use a batten to scribe between those points ....

>>> enough white micro balloons

mixed into the epoxy to make it creamy

about 5% to 10% of the epoxy weight !

you will have to try this out

since it will be different for every glass bubble typ

and epoxy system

will not only make it tougher but lighter as well !

it then weighs about half as much as water

so this is our general > glue < for building the vfp ....

when fiber glassing you put in a little less micro balloons

about 5% per weight

so the > mixture < will flow still better

then epoxy alone

and be still lighter as epoxy itself !

when we need a > structural mixture <

we put as well micro balloons into

about 5% per weight

and about 20% fiber cuts about 1/8" in lenght per weight

to have like a fiber glass at the end

if you want to use cotton fibers you have to build in the desert

at 10% humitity

or heat it up in the ofen at 300f before mixing it into the epoxy

since other wise it will have soaked up the water from the air

and will make a weak epoxy  system

the same for the redisch brown phenolic micro balloon typ

that has no place on a vfp

since it only advandage is its easy shaping !